## Slide 1: Monoclonal antibody capture using affinity complexation
1
BRX
+
Cell retention
Wash
Drain
Drain
Low pH
Membrane
Membrane
Regeneration
mAb rich
mAb depleted
Affinity
Reagent
SPTFF
HCP, DNA…
HCP, DNA…
Eluted mAb
Reconditing Buffer
Impurity Wash
Elution
Affinity reagent

## Slide 2
Properties of Successful mAb Affinity complex
Size
100 nm-5 μm
< 5x Elution MWCO (non-mAb components)
Binding, Elution
High capacity (mg mAb/mg NP)
Precipitating
Reversible
Sustainability, Cost
Soluble Expression
  Assembled and Folded
High Yield
Time (process speed)
PMI
Stability
Low pH stable
Salt stable
Non aggregating
Notes: Nanoparticle viability for continuous ultrafiltration is dependent on several key metrics:
Low pH stability
Solubility when bound to mAb
High binding capacity
Robust expression (E. coli)
Reliable and agnostic purification
Talk about how these properties Lead to our constraints for expression and design
Filtration process itself forces us to target a large particle size,
Binding/elution constraints require broad pH stability
Cost reduction requires affordable and speedy production
Stable to unbind form the mAb at conditions that are stable for the NP and the mAb. Fragmentation of NP can prevent its separation from the mAb.

## Slide 3: Methodology for screening mAb Affinity complex Spin filter test
100
75
50
100
75
50
2000 x g
<=50 uL
+
450 uL
Buffer
mix
100
75
50
2000 x g
<=50 uL
100
75
50
500 uL
100
75
50
L
F1
F2
R
+
50 uL
SDS-PAGE buffer
Rinse filter by pipetting
100
75
50
W
L
F1
F2
R
W
Successful enrichment in retentate denotes a functional capture of bioparticle
Crucial first test of feasibility for each conception of the system

## Slide 4: Initial mAb Affinity complex showed [mAb] dependence
L
F1
F2
R
W
A Mix at 4.3 mg/mL
B Mix at 0.81 mg/mL
C Mix at 0.43 mg/mL
D Mix at 0.25 mg/mL
Increase in mAb concentration was linked to higher retention of bioparticle. We determined that improvements should decrease concentration dependence and maximize % retained.
Preferred operating range
Retention>80%
Target 95%
Target 5%

## Slide 5: mAb Affinity complex B and C are more concentration independent and Show higher overall retention
Decreased concentration dependence and increased retention are proxies for improved performance over capture
Curves gives insight into formation and structure of mAb-bioparticle system
Compare different conceptions of the system at screening stage.
Target 95%

## Slide 6: Upcoming Challenges
Measuring Particulate Size Distribution
Controlling Particulate Size (peak)
Controlling Particulate Size (breadth)
Understanding Fluid Dynamics of Particulate Suspension
Controlling Particulate self-interaction
De-risking Particulate Membrane Interactions
Controlling Particulate Flow
Silva, R.C. Experimental Characterization Techniques for Solid-Liquid Slurry Flows in Pipelines: A Review. Processes 2022, 10, 597. https://doi.org/10.3390/pr10030597
Desired state
High self-interaction
Low self-interaction